## Slide 1: MIX DESIGN

## Slide 2: Concrete Mix Design
Wet Cast (Slump)

## Slide 3: Concrete Mix Design
Wet Cast (Slump)

## Slide 4: Concrete Mix Design
Dry Cast (no Slump)

## Slide 5: Concrete Mix Design
Dry Cast (no Slump)

## Slide 6: Concrete Mix Design
Combination of Art and Science…

## Slide 7: Water, Cement, & Aggregate
As the water to cement ratio increases, the strength of a concrete mix decreases.

## Slide 8: Water, Cement, & Aggregate
As the water to cement ratio increases, the strength of a concrete mix decreases.

## Slide 9: Water, Cement, & Aggregate
As the surface area of the aggregate increases more water will be needed to maintain a given slump.
    Coarser Surface Texture
    Particle Shape

## Slide 10: Water, Cement, & Aggregate
As the surface area of the aggregate increases more water will be needed to maintain a given slump.
    Particle Size Distribution

## Slide 11: Water, Cement, & Aggregate
As the surface area of the aggregate increases more water will be needed to maintain a given slump.
    Particle Size Distribution

## Slide 12: Water, Cement, & Aggregate
As the air content increases, the strength of the concrete decreases.

## Slide 13: Water, Cement, & Aggregate
As the air content increases, the strength of the concrete decreases.

## Slide 14: Water/Cement Ratio
It’s a calculation:
  w/c ~ lbs. of water / lbs. of cement
=
Water cement ratio
= 45 lbs ÷ 100 lbs
45 lbs of water
100 lbs of cement
= 0.45 expressed as decimal

## Slide 15: Water/Cementitious Ratio
It’s a calculation:
  w/cm ~ lbs. of water / lbs. of cementitious
=
Water cementitious ratio
= 45 lbs ÷ (80lbs + 20 lbs)
45 lbs of water
80 lbs of cement
= 0.45 expressed as decimal
+
20 lbs of Flyash

## Slide 16: Water/Cementitious Ratio
Often when w/c is discussed its really w/cm that is intended as the reference
Water/
Cementitious
Water/Cement

## Slide 17: Water/Cementitious Ratio
Water needs to be drinkable or meet ASTM 1602

## Slide 18
Specific Gravity
  The relative density of a material compared to water
  The ratio of a material’s weight to the weight of an equal volume of water
Terminology
Notes: 18

## Slide 19: Specific Gravity
What about you?
Notes: 19
Ratio of same volume to compare mass.
As if the stone was a solid block, not individual stones
Human specific gravity is very close to 1. If you float in water, it would be < 1

## Slide 20: Specific Gravity
Stone: Specific Gravity = 2.70
Water: Specific Gravity = 1.00
Same Volume, but 2.70 Times More Mass
Cement – 3.15
Steel – 7.85
You - ???
Notes: 20
Ratio of same volume to compare mass.
As if the stone was a solid block, not individual stones
Human specific gravity is very close to 1. If you float in water, it would be < 1

## Slide 21
Bulk Specific Gravity (SSD):
  Used to determine the “solid volume” (absolute volume) of a material going into concrete
  It is determined by submerging the material in water for 24 hours in order to fill any permeable voids
Terminology
Notes: 21

## Slide 22: Calculations for SSD Bulk Specific Gravity
Coarse Aggregate Using Basket Suspended in water:
B / (B - C) = SSD Bulk Specific Gravity
where:
B = weight of SSD sample in air
C = weight of SSD sample in water
Notes: 22

## Slide 23: Calculations for SSD Bulk Specific Gravity
Field Calculation of SSD Bulk Specific Gravity:
Weight of Aggregate @ SSD
Weight of equal volume of water displaced
=
Specific Gravity
1245g of SSD aggregate
=
469.81g of water displaced
2.65
Notes: 23

## Slide 24
Concrete Mix Design
  It’s always about volume!
  What is absolute volume?
Notes: 24

## Slide 25: What is Absolute Volume?
Relationship of Materials to Volume
  specific gravity of Type I Cement = 3.15
  specific gravity of water = 1.0
  1 gallon of water weights 8.33 pounds
  water weights 62.4 pounds / cubic foot
Pounds of Material
S.G. X 62.4
= Absolute Volume

## Slide 26: Basic Concrete Mix Design

## Slide 27: Basic Concrete Mix Design
667
3.15 X 62.4
1590
2.60 X 62.4
1242
2.65 X 62.4

## Slide 28: Basic Concrete Mix Design
Lbs Material
S.G. x 62.4
= Absolute Volume
= Lbs. of Material
S.G. x 62.4 x Abs. Volume

## Slide 29: Basic Concrete Mix Design
300
1.0 X 62.4
0.055 X 27

## Slide 30: Basic Concrete Mix Design
36 gal
1.0 X 62.4
36 Gal

## Slide 31: Basic Concrete Mix Design
36 gal x 8.33 lbs/gal
1.0 X 62.4
36 Gal

## Slide 32: Water/Cement Ratio = W/C
Water / Cement
300
667
Weight (mass)
Notes: 32

## Slide 33: Density (Unit Weight)
Design (unit weight)
3799
27.0
@ 1.5% air, unit weight (density) = 147.26
Notes: 33
The unit weight shown with 1.5% air is based on adjustments of the rest of the materials to maintain 27 cubic feet.

## Slide 34: Mix Design with Cement & Fly Ash
133 lbs. fly ash
667 Total lbs. Cm
= 20% ash
It’s about volume!
Notes: 20% fly ash is based on 20% by weight not volume.
The “Note” is usually true, but not always. Also note the change in w/cm ratio due to lower water demand.
34

## Slide 35: Mix Design with Cement & Fly Ash
It’s about volume!
Note: lower water
demand due to fly ash
- for same slump
Notes: 20% fly ash is based on 20% by weight not volume.
The “Note” is usually true, but not always. Also note the change in w/cm ratio due to lower water demand.
35

## Slide 36: Mix Design with Cement & Fly Ash
Proportion the mix to
yield 27 ft3 … but how
much sand, stone …
what ratio?
Sand / Aggregate
ratio is by volume
It’s about volume!

## Slide 37: Mix Design with Cement & Fly Ash
It’s about volume!
Volume without
aggregate = 8.72
27.00 - 8.72 =
18.28 ft3 required

## Slide 38: Mix Design with Cement & Fly Ash
It’s about volume!
Left for aggregates
Already used
27 ft³
8.72 ft³
18.28 ft³
18.28 ft³ + 8.72 ft³ = 27 ft³

## Slide 39: Sand to Aggregate Ratio
Volume of Sand
Volume of Total Aggregate
=
Manufactured Concrete Pipe
60-80% Packerhead Mix
45-65% Dry Cast
Rules of thumb ?
Notes: Chart is a blended gradation curve based on % retained
Percentages shown are a broad start and encompasses percentages for both volume and weight
39

## Slide 40: Calculating Sand & Stone to Yield 27ft3 of Concrete
Assume this concrete needs to have Sand / Aggregate ratio of 0.42
Volume of Sand = 7.68 ft3
Total Volume of Aggregate
= 0.42
Volume of Sand
Volume of Sand
18.28
= 0.42

## Slide 41: Calculating Pounds of Sand
Pounds of Material
S.G. X 62.4
= Absolute Volume
Pounds of Material (Sand)
2.65 x 62.4
= 7.68 ft³
Sand = 1270 lbs
Evert Sand S.G. = 2.65

## Slide 42: Calculating Volume of Stone
Total Volume Left for Stone
Sand Volume
= 10.60 ft³
18.78
- 7.68
Total Aggregate Volume
Notes: 42

## Slide 43: Calculating Pounds of Stone
Pounds of Material
S.G. X 62.4
= Absolute Volume
Pounds of Material (stone)
=10.60 ft³
Stone = 1720 lbs
Miller Stone S.G. = 2.60
2.60 x 62.4
Notes: 43

## Slide 44: SSD Mix Design

## Slide 45: Aggregate Moisture
Notes: 45

## Slide 46: Aggregate Moisture
Absorbed moisture
(absorption)
Free moisture
(moisture content)
SSD (ideal)
Add Water
Subtract
Water
Notes: 46

## Slide 47: Moisture Adjustments
Moisture Management is Critical (How much free water)
Total aggregate moisture = Aggregate absorption + Free water
Notes: Convert 26 & 59 Lbs into gallons for clarity to students
47

## Slide 48: Moisture Adjustments
Moisture Management is Critical (How much free water)
Aggregate Absorption = Total aggregate moisture - Free water
Notes: Convert 26 & 59 Lbs into gallons for clarity to students
48

## Slide 49: Moisture Adjustments
Moisture Management is Critical (How much free water)
Free Water = Total aggregate moisture - Aggregate absorption
Notes: Convert 26 & 59 Lbs into gallons for clarity to students
49

## Slide 50: Moisture Adjustments
What if we do not make moisture corrections
Notes: Convert 26 & 59 Lbs into gallons for clarity to students
50

## Slide 51: Moisture Adjustments
Moisture Management is Critical (How much free water)
Total aggregate moisture = aggregate absorption + free water
3.0% = 1.5% + free water,
0.015 X 1720 =
Stone
5.5% = 0.85% + free water,
  0.0465 X 1270 =
Sand
(% free water = 1.5%)
(% free water = 4.65%)
26 pounds of free water on the Stone
59 pounds of free water on the Sand
Notes: Convert 26 & 59 Lbs into gallons for clarity to students
51

## Slide 52: Moisture Adjustments
Moisture Management is Critical (How much free water)
Total aggregate moisture = aggregate absorption + free water
Notes: Convert 26 & 59 Lbs into gallons for clarity to students
52

## Slide 53: Water Adjustment
If 26 + 59 pounds of water rides in on the aggregates
you must take that amount of water out of the BATCH water.
Design water
Water on aggregates
Batch water
295
-85
210
Notes: 53

## Slide 54: Moisture Adjustment
Total moisture = Free moisture + Aggregate absorption
SSD & batch totals
will be the same
Notes: Circled numbers above should be the same because of the moisture adjustment.
Note that Batch Weights have been increased from the SDD Aggregates
54

## Slide 55
Where Can I Get This?
Portland Cement Association (PCA)
  5420 Old Orchard Road
  Skokie, IL 60077-1083
  847 966-6700 PH
  847 966-8389 FX
  Info @ cement.org