## Slide 1: Concrete Production

## Slide 2: Concrete Production
ASTM C94 - why?
Specifications for ready mix most closely align with our product mix and production concepts
Good starting point for specifications rather than inventing new ones
Notes: C94 if for ready mix concrete. May not apply to dri-cast mixes. Check your local agencies for any specific tolerances

## Slide 3
Redi-mix Requirements
Consistent Aggregates
Aggregates Stored Properly
Accurate Mix Proportions
Consistently Mixed
Transported to the forms

## Slide 4: Concrete Production Topics
Material Handling
Batching
Mixing
Transporting

## Slide 5
Material Storage
And
Handling

## Slide 6
Minimize Segregation
Do not store in conical piles
Store in horizontal layers
Prevent Contamination
Store on slabs or planking
Have storage bins separated by walls
Keep gradations within specified limits
Reference ACI 304, “Guide for Measuring and Placing Concrete”
Proper Aggregate Storage
Notes: Horizontal layers = bunker storage as seen in the following slide
If stored on ground, loader may dig into dirt contaminating the aggregate

## Slide 7
Notes: Picture shows a lot very fine material. Conical piles good practice?

## Slide 8
Stockpiles that stack traditionally can segregate, with coarser material falling to the bottom/outside, and finer material remaining in the center and top. Degradation can occur if loaders or dozers drive onto the stockpile, or if material is falling from a great height — potentially splitting or crushing the gradated material. Equipment driving on stockpiles can also cause contamination,
as it tracks dirt or loose material onto the stockpile.
Notes: Tell how barges are loaded and how the larger rock falls to the far side

## Slide 9
WOW!

## Slide 10
Correct loading techniques gathers a blend and does not hurt the pile
Flat Stacks

## Slide 11
Notes: Caution:
Scooping water
Walls high enough to not cross contaminate

## Slide 14
Under the individual grizzlies will be a system similar to this. The storage bins are directly under the truck dump areas and feed into individual weigh hoppers or onto a cumulative weigh belt that leads to the mixer

## Slide 16
Filling Aggregate Bins
Correct
Incorrect
Notes: Material can segregate in agg bins

## Slide 17: Batching

## Slide 18: Batching
Accuracy of weighing
Compensating for moisture in Aggregates
Sequencing

## Slide 19: Typical Batching Tolerances (C94)
Cementitious +/- 1%
(for batches less than 1cy not less than required, up to 4% over)
Water +/- 1%
Fine Aggregates +/- 2%
Coarse Aggregates +/- 2%
Cum. Aggregates +/- 1%
Admixes +/- 3%
(or minimum recommended dosage per 100 weight or which ever is greater)
Notes: C94 is for Ready mix concrete. May not apply to dry cast mixes. Check your local specs

## Slide 20: Accuracy
Scales must hang free
Scales (gates or valves) must not leak
Scales must empty completely after each batch
Zero on scales should be checked on a regular basis
Calibrate scales annually
Notes: Mention venting of cement and fly ash

## Slide 21: Why Compensate for Moisture in Aggregates?
Batch Consistency
Predictable strengths
Production efficiency

## Slide 22
The free moisture must be accounted for when batching our concrete to help control mix costs and to improve its quality and consistency
Free Moisture
Notes: Probes are used for 2 reasons:
in aggregate bin, compensates for weight of the aggregate
in mixer, compensates for the weight of the water

## Slide 23
Consider the amount of water in 1,854 pounds of sand
(which is a typical amount of sand for a yard of pipe machine concrete)
that has 4% total moisture in it and has an absorption of 1%
This gives us free moisture of 3% (4%-1%)
Free Moisture Example
Notes: Probes are used for 2 reasons:
in aggregate bin, compensates for weight of the aggregate
in mixer, compensates for the weight of the water

## Slide 24
At 3% moisture:
The 1,854 pounds of sand that we weighed up is 1800 pounds of SSD sand and 54 pounds of water
Fifty-four pounds of water is 6 ½ gallons (54pounds/8.33 pounds per gallon) of water
We are 54 pounds short of sand and we have 54 extra pounds of water
If we do not compensate properly for this difference, it will significantly affect the cost and quality of the concrete that we are producing
Free Moisture Example
Notes: Probes are used for 2 reasons:
in aggregate bin, compensates for weight of the aggregate
in mixer, compensates for the weight of the water

## Slide 25
  The old fashioned way
  Water Valve (hose)
  No compensation for lost (yield) aggregate
  Inconsistent mixes (slump)
  Inconsistent strengths due to varying batch proportions and W/Cm ratio
Compensating for Moisture in Aggregates
Notes: Emphasize moisture control is necessary for consistent mixes

## Slide 26
Daily burn offs of aggregate samples
  Compensation for moisture in aggregates remains constant as long as moisture does not change between burn offs
  Can improve batch consistency (slump)
  Can improve strength consistency
Compensating for Moisture in Aggregates without Probes

## Slide 27
Moisture Probes
  Good batch consistency (Slump)
  Automatic compensation for Aggregates
  More consistent strengths
  Probes need to be calibrated and calibration must be checked on a routine basis based on requirements from your local agencies.
Compensating for Moisture in Aggregates
Notes: Probes must be calibrated
Probes should be used in at least the sand and if possible in the coarse aggregate. If not in coarse ag, then it must be oven dried.
Probes measure total moisture, not free moisture

## Slide 28: Microwave Bin Probe Calibration Plots
Typical Sand Microwave Bin Probe Plot

## Slide 29
Typical Rock Microwave Bin Probe Plot
Microwave Bin Probe Calibration Plots

## Slide 30
Shifts in Probe Calibrations
Microwave Bin Probe Calibration Plots

## Slide 31
Aggregates
Cementitious
Water
Admixtures (per admix manufacturer recommendation)
Aggregates
Water
Cementitious
Admixtures (per admix manufacturer recommendation)
OR
Sequencing (per manufacturer’s recommendation)

## Slide 32
Depends on Mixing system
Generally cement should be discharged when all aggregates and water are in mixer
If cement balling occurs cement should be discharged sooner or later depending on your mixer
Ask your mixing manufacturer for a recommended sequence and timing schedule
Sequencing Cement

## Slide 33
Mix Consistency
Reducing the amount of additive added (cost)
How it affects the probe readings
Why does the Sequencing of Admixtures matter?

## Slide 34
Air entraining should be added with the mix water or aggregates
Air entraining should be mixed with aggregates for a few seconds before adding cement
Air Entrainment Sequencing

## Slide 35
Should be added with the aggregates and water
Lubricant/Surfactant Sequencing (Dry Cast)

## Slide 36
Water Reducers should be added with the mix water after the air entraining is done
Water Reducer Sequencing

## Slide 37
High Range Water Reducers should be added at the end of the batch after all ingredients are thoroughly mixed
High Range Water Reducer (Super/Superplasticizer) Sequencing

## Slide 38
Always work with your admixture supplier when you have batching sequence questions or issues
Admixture Sequencing

## Slide 40
It is important to understand the effect of time on your concrete. The workability and quality of the concrete will deteriorate particularly in hot weather

## Slide 42: Mixers

## Slide 43
Quantity of concrete needed per day
Quantity of concrete needed per hour
Mixer Output

## Slide 44
Output is measured in:
    ft3
    yd3
    m3
  Typically 2/3 of rated capacity!!!
Mixer Output
Notes: It’s 2/3rds because the raw ingredients take more room than the mixed result. Some mixers will mix the rated capacity (ie…Skako)
Have them ask what the min and max output capacity

## Slide 45
Paddle Mixers
Ribbon/Spiral Blade Mixers
Pan Mixers
  Counter-Current
    Rotating Pan
    Stationary Pan
Twin-Shaft Mixers
Common Types of Mixers

## Slide 46
PADDLE MIXER
Notes: Paddle mixer
If you are going to use a lab mixer for trial batching, you would probably use this type of mixer.

## Slide 47
RIBBON MIXER
Notes: Spiral blade or ribbon mixer

## Slide 48
TURBINE MIXER
Notes: Turbine pan mixer

## Slide 49
COUNTER CURRENT MIXER
Notes: Counter current mixer

## Slide 50
PAN MIXER

## Slide 51
TWIN SHAFT MIXER
Notes: Twin Shaft

## Slide 52: Concrete Transport

## Slide 54
Discharge into center of bucket or hopper
Incorrect
Correct
Concrete Discharge from Mixer

## Slide 55
Avoid
  Segregation
  Loss Of Mortar
  Loss of Slump
Handling Concrete

## Slide 56
Most common cause of damage occurs:
  if concrete is not discharged vertically
  at free-fall distances more than 6 feet
  when jarring or shaking during transportation
Open chutes
  more than 20’ Long
  chutes that are too steep (slide not tumble)
Segregation
Notes: 6-10’ is acceptable due to the fact that producers are pouring 8’ lengths, but the closest possible is best

## Slide 57
Place concrete in the form near its final location
Keep free-fall to a minimum
Use flat forms
  Begin pour at corner or edge
  Pour in equal lifts
Vertical Forms
  Pour in horizontal layers
  For large blockouts, pour on one side - allow concrete to flow underneath
Pouring Concrete
Notes: Blockouts: pour from one side to avoid trapping air by pouring from both sides.

## Slide 58
Questions?
Tom Umek
Tom.Umek@cam-hp.com