## Slide 1: Curing

## Slide 2: Curing
Hardening of concrete
Hydration CSH gel
Accelerated curing
  The rate of hydration increases as the ambient temperature increases
Maintaining moisture in the concrete is critical
Notes: Curing is more than the hardening of concrete
Hydration is not a “drying out” of concrete but rather a chemical reaction

## Slide 3
Reduces permeability
  Essential for structure watertightness
  Improves durability
Optimal strength achieved
Proper Curing is Essential

## Slide 4
Maintain moisture
Maintain temperature
Essentials for Proper Curing

## Slide 5
Notes: What’s wrong here: product covered, but there is a rip in the plastic. No moisture added, and therefore being cured in a dry atmosphere which can’t be done with exposed concrete.

## Slide 6
Proper moisture and temperature result in increased concrete strength
Concrete Strength
vs
Moisture Condition
Notes: If moist cured (water bath), you will get 100% design strength at 28 days. (Note: the difference in moist and air cured is generally not as severe as show in this graph, but it should be explained that there is some loss of strength)
Explain that if they put a piece on the plant floor and throw a tarp over, they will notice water on the inside of the tarp…therefore if not covered, that water is just escaping…Suggest at least covering product

## Slide 7
Compressive Strength
% of 28 day
73°F(23°C) concrete
Low Temperature
vs
Strength
Notes: Show the lower temps = lower strengths…most pipe producers are curing at 120 degrees. The 120 degree line would show a higher early strength, but lower final strength.

## Slide 8
Maintaining moisture by wetting
Prevent moisture loss by sealing
Accelerated curing
Curing Methods

## Slide 9
Wet burlap
Spraying/Misting
Fogging
Maintaining Moisture by Wetting
Notes: Recommended by Mel to fog during the day while hot
Mention: If burlap is not kept wet, it will wick away moisture and hurt you more than helping

## Slide 10
Cold or hot
Very fine droplets
Air pressure
Effective for higher cement content and warmer climates
Spraying/Misting
Notes: Caution: If using a Jay Bird, they must be high enough to avoid air movement that will crack the pipe.
Water should also be proper temperature to avoid cracking the pipe if the water is too cold.

## Slide 11
Forms
Tarps / Polyethylene
Curing Compounds
  Caution:
    If w/c <0.5
    With pozzolanic mixes
Prevent Moisture Loss by Membrane Sealing
Notes: If wet casting at least cover the ends
If a curing compound is NOT membrane forming, there is a potential for moisture loss
Ask Mel about the Caution on pozzolanic mixes

## Slide 12
Dry Heat
  Use with caution: difference between accelerated curing and maintaining heat
  Heated beds (hollow core)
  Electric or gas heaters – convection heat
  Infrared heating – radiant heat
Low pressure steam
  Boilers
  Steam generators
Admixtures
Note: Raise concrete temperature while maintaining high humidity
Accelerated Curing
Notes: Admixes accelerate the set or strength gain, but are not a substitute for proper curing environments

## Slide 13
2 Classes of Admixtures:
  Set Accelerator
  Strength Accelerator (Early Age)
Calcium Chloride is the most common in Ready mix, but BEWARE should not be used in precast reinforced concrete
Several non-chloride, non-corrosive accelerators, but generally most are not as effective as calcium chloride
Accelerating Admixtures
Notes: Calcium Chloride is not recommended for use in reinforced concrete due increased corrosion of the reinforcement in its presence.

## Slide 14
As a rule of thumb, a temperature increase of 18F doubles rate of hydration
High temperatures with low humidity can crack the product
The lower the curing temperature, the longer the product must be cured to achieve comparable early strengths
Considerations for Accelerated Curing

## Slide 15
Notes: Higher the temp = higher the rate of hydration
Note: Type IV is not commercially available

## Slide 16
Notes: Example of poor curing because no moisture is being maintained or added.

## Slide 17
Notes: One method to use radiant heat while maintaining moist curing environment…Just an example, but is expensive

## Slide 19
Notes: Live steam is most common providing both the heat and the humidity

## Slide 20
Provides both heat and humidity
Product is heated by the warmer steam condensing on it
Moisture evaporation is minimized
Low Pressure Steam Curing

## Slide 21
Notes: Curing showing a relative strength for a given amount of time and temperature. i.e. Higher the temp, faster the curing for the same strength.
Caution students to not cure above 160 degrees per ASTM

## Slide 22
Preset (< 90 degrees) – at least one hour
Ramp (Temperature Rise) – at 20F to 40F per hour
Hold / Soak (at target temperature) – varies with the product
Cool Down
Typical Accelerated Steam Curing Cycle
Notes: Mel uses the I-button at this time to show one way to monitor curing temps.
Determining preset times for dry cast is very difficult. Preset could be 5 hours, but note that at least 1 hour…The longer the preset, the better the product will be. Historically, a preset of 1 hour has proven to be effective for products cured in kilns.
Must test product to know how long to “hold” product to be most efficient

## Slide 23
1) Preseting
2) Ramping
3) Holding
4) Cooling
Idealized Accelerated
Steam Curing Cycle

## Slide 24
Concrete product temperature = Kiln air temperature
Concrete product no longer gains weight from the moisture condensing on its surface
Concrete begins to lose weight to the kiln atmosphere
Generally, the equilibrium temperature is higher for less dense production
Target or Equilibrium Temperature

## Slide 25
Notes: Equilibrium Temp = temp where it no longer gains or loses moisture
DEF problems occur when concrete temp shoots up above the curing cell temp

## Slide 26
Concrete Pipe (Typical for Accelerated)
  120 F to 140 F (50º C to 60º C)
  4 to 6 hours
Precast (including Pipe)/Prestress limits (ACI)
  160 F (71 C) in Canada
  160 F (71 C) in USA
  8 to 12 Hours
Concrete Target Temperatures
Notes: Note: these are concrete temps, not air temps

## Slide 27
Leave forms on as long as possible
Check with supplier when using accelerated admixtures
Wet Cast Products

## Slide 28
Require 90 to 100% humidity
Must protect from drafts
Dry Cast Products

## Slide 29
Hot weather curing
  Shade, sprinkle coarse aggregates
  Add ice to mix water or use water chiller
  Shelter product from direct sunlight
Special Conditions
Notes: Chillers are great, but if using a low w/c, there isn’t much water to cool.
When using ice, use crushed if possible

## Slide 30
Cold weather curing
  Keep fresh concrete temperature > 50F
  Heat aggregates
  Heat water
Special Conditions
Notes: If you need (by using chart) to heat the water over 160 degrees, heat aggregate as well.

## Slide 31
Notes: If you need (by using chart) to heat the water over 160 degrees, heat aggregate as well.

## Slide 33
Determine actual curing cost
Review curing cycle
  Preset, ramp, hold
Curing chambers
  Insulation, partitions, canopies
Prevent flueing
  Direct steam flow out curing cell bottom only
  No steam leakage along the sides or through the top
Reducing Energy Costs
Notes: Qcast REQUIRES that you monitor what happens in the curing cell

## Slide 34
Notes: Pic showing a plant who couldn’t get temp…this shows the problem of energy and stem being released out the top.

## Slide 35
Notes: Should only see stem coming out the bottom. If they are having problems, put hand over any holes to see if heat is escaping. Or put a match or cigarette or match under tarp…If smoke goes up, then there is flueing problems.

## Slide 36
Conclusion: Want smoke flowing out of cell

## Slide 37
Light a match
  Flame flows in if Flueing
If the floor of the cell is cold and dry
  Cold air pulled into the cell
  Flueing.
If the floor is warm and wet
  Steam flowing out of the kiln bottom
  Not flueing
Additional checks for Flueing

## Slide 38
www.maxim-ic.com ---- iButton
800-336-6933
DS1921K - starter kit
DS19216 – extra button

## Slide 39
Questions?
Mel Marshall
Mel@mcmconultants.ca