## Slide 1: PRODUCT TESTING

## Slide 2: Learning Objectives
Provide an overview of pipe testing requirements and procedures for ACPA Certification and understand why we need to do the tests.

## Slide 3: PIPE TESTS
External load crushing strength test (Three-Edge Bearing test)
Joint shear test
Off-center joint test
Storm sewer and culvert joint test
Water tightness tests
ACPA QCast Plant Certification Manual provides specific detail of testing requirements

## Slide 4
Notes: calculated based on laying length of the pipe, not the testing board length

## Slide 6: THREE-EDGE BEARING TESTING
Understand what you are doing
Understand why you are doing it

## Slide 7: REQUIRED READING:
ASTM C497 - Standard Test Methods For Concrete Pipe, Concrete Box Sections, Manhole Sections, or Tile:
  Section entitled - External load crushing strength test by the three-edge bearing test method
ASTM C76 –Standard Specification for Reinforced Concrete Culvert, Storm Drain, and Sewer Pipe:
  Tables 1-5 provide strength requirements

## Slide 8: ASTM C76 –Standard Specification for Reinforced Concrete Culvert, Storm Drain, and Sewer Pipe: Tables 1-5 provide strength requirements

## Slide 9: WHY DO WE RUN THE THREE-EDGE BEARING TEST? To determine the strength of our pipe using two different criteria:
A. The load to produce a crack with a width of 0.01”
B. The ultimate load

## Slide 10: D-LOAD Pounds per foot of length per foot of diameter
For example: ASTM C76 Class III design
D-load to produce a 0.01” crack 1350 D-load to produce the ultimate load 2000

## Slide 11: SAMPLE CALCULATIONS FOR 24” DIAMETER x 8’ CLASS III PIPE
0.01” load = 1350 (D-load) x 8 ft (length) x 2 ft(diameter) = 21,600 lbs.
Ultimate load = 2000 (D-load) x 8 ft. (length) x 2 ft (diameter) = 32,000 lbs.

## Slide 12
1” – 1 ½”
Notes: Point out critical elements and that they should be straight and stiff to get a more favorable result
To your advantage to use max spread of bottom edges

## Slide 13: Load Rate
ASTM C497
For Reinforced Concrete Pipe, any rate of load application up to a maximum of 7500 lbf/lineal foot of pipe per minute shall be used up to 75% of the specified design strength, at which time the rate of loading shall be reduced to a maximum uniform rate of 1/3 of the specified design strength of the pipe per minute.

## Slide 14: Loading Rate for TEB Testing
7500 lbf/LF/min
1/3 design strength/min

## Slide 15: Load Rate Calculation Example
Test Class III, 24 in. pipe, 8’ long
{ASTM C76} 0.01” load = 1350 (D-load) x 8 ft (length) x 2 ft (diameter) = 21,600 lbs
  75% of 21,600 lbs is 16,200 lbs.
Maximum Rate up to 75% is 7500 lbf/lineal foot of pipe (8’) per minute
  7500*8’= 60,000 lbs/minute / (60s/min) = 1,000 lbs/sec
  16,200 lbs / 1,000 lbs/sec = 16 seconds
  Minimum 16 seconds to reach 16,200 lbs.

## Slide 16: Maximum Loading Rate for TEB Class III, 24 in. pipe, 8’ long
Seconds
16,200 lbs in not less than 16 sec.
21,600 lbs
75 %

## Slide 17: Load Rate Calculation Example (cont.) Class III, 24 in. pipe, 8’ long
After 75% - reduce rate to 1/3 design strength / minute
  1/3 of 21,600 lbs = 7,200 lbs/minute / (60s/min) = 120 lbs/sec
  Max rate of 120 lbs/sec between 16,200 lbs and 21,600 lbs.
  Time equals 21,600-16,200 [5,400 lbs] / 120 lbs/sec = 45 seconds.
  Total test time equals 16 secs + 45 secs = 61 seconds minimum
  At least one minute but depends on pipe size and class.

## Slide 18: Maximum Loading Rate for TEB Class III, 24 in. pipe, 8’ long
Seconds
21,600 lbs
75 %

## Slide 19
D-Load Rate Calculator
Found On The ACPA Member’s Website:
Q-Cast Tools

## Slide 20
Notes: ACPA Website has a lot of great tools for you to use

## Slide 21
“…when the point of the gage will, without forcing, penetrate 1/16” at 3 in. maximum intervals throughout distance of 1 ft.”

## Slide 22
Notes: It’s 3-edges, not 3 points

## Slide 23
Notes: Should be tested that pipe is set squarely in the machine

## Slide 25
ACPA QCAST MANUAL
T.E.B. TEST FREQUENCIES
PIPE SIZE CLASS FREQUENCY 12”-15” Class 5 and below 1/1000 pcs. 18”-36” Class 4 and below 1/800 pcs. 18”-36” Class 5 1/400 pcs. 42”-60” Class 3 and below 1/400 pcs. 42”-60” Class 4 and 5 1/200 pcs. 66” and All classes As required larger by project specs.

## Slide 26: Pipe shall be tested to the D-load specified in the ASTM tables for the 0.01-inch crack. Pipe meeting these requirements shall be accepted for use. ACPA requires: one piece, per size and class produced, shall be tested to the Ultimate D-load at least one per year.
ACPA T.E.B. TEST FREQUENCIES

## Slide 28: JOINT SHEAR TEST
SPECIFIED IN ASTM C497
SANITARY CERTIFICATION ONLY

## Slide 29
SANITARY

## Slide 30: JOINT SHEAR TEST REQUIREMENTS 4000 lbs/ft of pipe diameter (per ASTM C497) including the weight of the pipe.

## Slide 31: WHAT IS A PASSING TEST- Joint Shear? Load Joint to 4000 lbs/ft diameter Crack Width less than 0.01” after the load is released.

## Slide 32
Notes: Example of 1 method

## Slide 36: DOCUMENTATION A proof of design test for the lowest class of each pipe size and joint style should be retained on file as a permanent record.
Expect to run a joint shear test during the audit (sanitary) unless done at another company plant on same design (must be QCast certified).
Notes: Note the Appendix here that shows Auditor Requirements

## Slide 37: OFF CENTER JOINT TEST REQUIREMENTS
VACUUM or HYDROSTATIC
Proof of design test on file. All pipe sizes and joint designs
Sanitary Certification Requirement.

## Slide 38
SANITARY

## Slide 41: WHAT IS A PASSING TEST – Off-Center? (QCast)
Vacuum test: Less than 0.108” drop from 7 inches of mercury over set time period
Hydrostatic test: Maintain 13 psi for 2-1/2 minutes with no visible leakage (drips)
  [Can condition the pipes up to 24 hours.]
Test must be run during a (sanitary) audit unless testing performed at another company plant that is QCast certified.

## Slide 43: STORM SEWER AND CULVERT JOINT TEST REQUIREMENTS
Gasketed Storm Pipe Joints
VACUUM or HYDROSTATIC
Proof of Design for all Gasketed Pipe Sizes and Joint Designs

## Slide 45
Notes: Defined in 443

## Slide 46: WHAT IS A PASSING TEST –Gasketed Storm Joint Test (QCast)?
Vacuum test: Less than 0.108” drop from 7 inches of mercury over set time period
Hydrostatic test: Maintain 3 psi for 10 minutes with leakage rate less than 200 gallons/inch diameter/mile of pipe/24 hours

## Slide 47: WATER TIGHTNESS TESTS Sanitary Certification Requirement
In-plant quality control tests for pipe barrels
12”-36” pipe Vacuum or Hydrostatic (test 100%)
42” & larger pipe and manhole Vacuum or Hydrostatic
  (1/100, min. of 2 pieces)

## Slide 51: ACPA PIPE PLANT CERTIFICATION Requires 100% plant testing 12”-36” Sanitary Sewer Pipe
12”-36” Vacuum Test
  Starting vacuum is 7” Hg
12”-36” Hydrostatic Test
  13 psi for 2 1/2 minutes
Found in Appendix A of QCAST Certification Manual

## Slide 53
Notes: X-tech produces digital monometer

## Slide 58
OK to use modified Vacuum Test Pressures and Time,
see QCast Appendix

## Slide 59: 12” - 36” HYDROSTATIC (Water)
100% OF SANITARY PIPE
13 psi for 2 1/2 minutes
NO VISIBLE LEAKAGE THAT RESULTS IN A DRIP

## Slide 60: 42” AND LARGER HYDROSTATIC or VACUUM TEST
Hydrostatic test - 13 psi for 2-1/2 minutes with no visible leakage (drip)
Vacuum test per table
1/100 - minimum of two per lot
Notes: 36” must test 100% and 42” only 2, why? Because at some point the wall is thick enough, and ACPA has drawn the line at 42”

## Slide 61: QUESTIONS?