## Slide 1
Reinforcement 1
Jake Jyrkama, P.E.
Rinker Materials

## Slide 3: Purpose of Reinforcement
Concrete properties
  Strong in compression
  Weak in tension
Reinforcement supplies strength to withstand tensile and shear forces experienced by concrete

## Slide 4: Compressive Forces on Concrete
Concrete can withstand compression

## Slide 5: Concrete Under Compression
This 2” X 2” cube of concrete withstands a 4000 psi compressive force

## Slide 6: Tensile Forces on Concrete
Without reinforcement, concrete will fail in tension

## Slide 7: Concrete Under Tension
The same 2” X 2” cube of concrete fails under a 400 psi tensile force

## Slide 8: Non-reinforced Concrete Behavior

## Slide 9: Flexural Forces on Concrete
Without reinforcement, the bottom side will fail in tension

## Slide 11: Reinforced Concrete Behavior
CONCRETEPIPE.ORG

## Slide 13: Concrete Behavior Under Shear
Vertical Shear

## Slide 14: Concrete Behavior Under Shear
Horizontal shear
shear reinforcement

## Slide 15: Effectiveness of Placement

## Slide 16: 0.01” Crack in Pipe
DEFLECTION UNDER TEST CONDITION
STRESS ZONES UNDER TEST CONDITION
TENSION COMPRESSION

## Slide 18: EXAMPLE: Ø36” X 4” WALL
MOVING STEEL INTO WALL TO 1 ½” VS 1” COVER AND DUE TO CRACKING GEOMETRY
INCREASED STEEL BY 47%
DUE TO SHORTER d

## Slide 19: Ø36” X 4” WALL
AS d = RESISTANCE TO CRACK WIDTH
d. MIN. = 147 %
d. NOM. = 100%
d. MAX. = 77%
D- LOAD WOULD VARY BY 34%
IF WE USED THE
ALLOWED CAGE POSITION TOLERANCE FROM C76

## Slide 20: Box Culvert

## Slide 21: Steel Nomenclature
As1 = Sidewall outside face As2 = Top slab inside face As3 = Bottom slab inside face As4 = Sidewall inside face
As5 = Top slab inside distribution steel
As6 = Top slab outside distribution steel As7 = Top slab outside face
As8 = Bottom slab outside face

## Slide 22: Effectiveness of Placement
1” cover vs. 1-1/4” cover for various fill heights

## Slide 23: Effects of Increased Steel Cover
Reduced 0.01” strength
Reduced shear strength
Reduced radial tension strength
Increased cost
Waste of steel

## Slide 24: Effectiveness of Placement
It is critical to have correct steel placement for both pipe and box culverts

## Slide 25: Reinforcement Type and
Identification

## Slide 26: Reinforcement Types
Reinforcing bars
Reinforcing wire
Bar mats and welded wire fabric
Zinc or epoxy coated reinforcement
Prestressing and post tensioning
All types must meet “Buy America” Requirements for federally funded projects

## Slide 27: Reinforcing Bars
Conform to specifications
  ASTM A615 (New Billet)
  ASTM A616 (Rail)
  ASTM A617 (Axle)
  ASTM A706 (Weldable)
Other bars may be used if permitted by design
Mill certificates required for each shipment

## Slide 28: Grade 40 & 50 Rebar

## Slide 29: Grade 60 & A706 Rebar
4
4
4

## Slide 30: Steel Area Using Different Combinations of Bar Sizes and Spacing
Spacing | #4 | #5 | #6 | #7 | #8 | #9 | #10 | #11
2 in. | 1.20 | 1.86 | 2.64 |  |  |  |  | 
3 in. | 0.80 | 1.24 | 1.76 | 2.40 | 3.16 | 4.00 |  | 
4 in. | 0.60 | 0.93 | 1.32 | 1.80 | 2.37 | 3.00 | 3.81 | 4.68
5 in. | 0.48 | 0.74 | 1.06 | 1.44 | 1.90 | 2.40 | 3.05 | 3.74
6 in. | 0.40 | 0.62 | 0.88 | 1.20 | 1.58 | 2.00 | 2.54 | 3.12
7 in. | 0.34 | 0.53 | 0.75 | 1.03 | 1.35 | 1.71 | 2.18 | 2.67
8 in. | 0.30 | 0.47 | 0.66 | 0.90 | 1.19 | 1.50 | 1.91 | 2.34
9 in. | 0.27 | 0.41 | 0.59 | 0.80 | 1.05 | 1.33 | 1.69 | 2.08
10 in. | 0.24 | 0.37 | 0.53 | 0.72 | 0.95 | 1.20 | 1.52 | 1.87
11 in. | 0.22 | 0.34 | 0.48 | 0.65 | 0.86 | 1.09 | 1.39 | 1.70
12 in. | 0.20 | 0.31 | 0.44 | 0.60 | 0.79 | 1.00 | 1.27 | 1.56
13 in. | 0.18 | 0.29 | 0.41 | 0.55 | 0.73 | 0.92 | 1.17 | 1.44
14 in. | 0.17 | 0.27 | 0.38 | 0.51 | 0.68 | 0.86 | 1.09 | 1.34
15 in. | 0.16 | 0.25 | 0.35 | 0.48 | 0.63 | 0.80 | 1.02 | 1.25
16 in. | 0.15 | 0.23 | 0.33 | 0.45 | 0.59 | 0.75 | 0.95 | 1.17
17 in. | 0.14 | 0.22 | 0.31 | 0.42 | 0.56 | 0.71 | 0.90 | 1.10
18 in. | 0.13 | 0.21 | 0.29 | 0.40 | 0.53 | 0.67 | 0.85 | 1.04

## Slide 31: Reinforcing Wire (Plain and Deformed)
Conform to (except prestressing wire)
  ASTM A1064
Other wire may be used if permitted by design
Mill certificates for each shipment

## Slide 32: Bar Mats and WWR (Plain and deformed)
Conform to
  ASTM A1064
Mill certificates for each shipment
Applications of rolled vs. straight

## Slide 34: Welded Wire Reinforcement

## Slide 35: Welded Wire Reinforcement

## Slide 36: Cage Basics
circumferentials
Spacing between pipe longitudinals
Area of one circumferen- tial wire (.025 sq. in.)
inal wire (.02 sq. in.)
Width of mesh – from top to bottom circumferential
W = Plain/Smooth, D = Deformed
Length of roll
3x8 W2.5xW2.0 93”x600’ 1/2x1/2
Overhangs
Spacing between pipe Area of one longitud-

## Slide 37: Wire Size and Designation
No. = Cross sectional Area in Hundredths of Sq. In.
Thus
  W5 = 0.05 Sq. In.
  W5.5 = 0.055 Sq. In.
  D10 = 0.10 Sq. In.

## Slide 38: Cage Basics
Given 3x8 W2.5xW2.0
What is the steel area per foot of pipe?
A = 0.025 x
3
12
= 0.10 in2/ft

## Slide 39: Structural Integrity Depends on
Grade of the reinforcing steel
Size of the reinforcing steel
Spacing of the reinforcing steel
Positioning of the reinforcing steel

## Slide 40: Thank You
Jake Jyrkama, P.E. Jaakko.Jyrkama@RinkerPipe.com