## Slide 1
CONCRETEPIPE.ORG
Reinforcement 2
Jake Jyrkama, P.E.
Rinker Materials

## Slide 2: Concrete Pipe Design
CONCRETEPIPE.ORG

## Slide 3: Structural Design
Indirect (D-Load) – (ACPA DD-9)
Designed for concentrated load (3-Edge Bearing Test) that will produce the same bending moments as in the field
Direct Design
Designed for the anticipated soil pressures using typical ultimate strength design methodology
CONCRETEPIPE.ORG

## Slide 4: Concrete Pipe Strength (ASTM C76/AASHTO M170)
D-Load
Supporting strength of a pipe loaded under three-edge-bearing test conditions
Expressed in pounds per linear foot per foot of inside diameter or horizontal span
ASTM C 76 Class IV D0.01 = 2,000
DULT = 3,000
CONCRETEPIPE.ORG

## Slide 5: ASTM C76
D-Load
CONCRETEPIPE.ORG
0.01”D
Ult. D
Class I | 800 | 1200
Class II | 1000 | 1500
Class III | 1350 | 2000
Class IV | 2000 | 3000
Class V | 3000 | 3750

## Slide 6: D-Load Strength Determination
48” Profile Class IV 8’ D0.01 = 2000
DULT = 3000
Total Load Required:
D0.01 = (48/12)(8)(2000) = 64,000 lbs DULT = (48/12)(8)(3000) = 96,000 lbs
CONCRETEPIPE.ORG

## Slide 11: Positioning Reinforcement
CONCRETEPIPE.ORG

## Slide 12: Positioning Reinforcement
CONCRETEPIPE.ORG

## Slide 16: Welding
CONCRETEPIPE.ORG

## Slide 17: Welding Requirements
Welding of reinforcement
Maintain product integrity
Two weldability limits
  Max. Carbon content (0.30%) [AWS D1.4]
  Carbon equivalent (CE)
ACI 318 And AWS D1.4, CE are:
  For #6 And smaller - 0.55%
  For #7 And larger - 0.45%
The lower The CE, The better The weldability
For larger CE values, The rebar must be preheated
CONCRETEPIPE.ORG

## Slide 18: ASTM A615 Reinforcement
ASTM A615 rebar
Must be used with extreme caution
Generally not acceptable
Check CE = %C + %Mn / 6
CONCRETEPIPE.ORG

## Slide 20: ASTM A706 Reinforcement
CONCRETEPIPE.ORG
ASTM A706 rebar
Is a low-alloy weldable grade
Check CE =
%C + %Mn/6 + %Cu/40 + %Ni/20 + %Cr/10 - %Mo/50 - %V/10

## Slide 22: Arc Welding
AWS D1.4

## Slide 23: Pre-Heating Guidelines
CONCRETEPIPE.ORG

## Slide 24: Fabrication
CONCRETEPIPE.ORG

## Slide 32: ACI 318 – Details of Reinforcement
Standard Hooks
Minimum Bend Diameters
CONCRETEPIPE.ORG

## Slide 33: Minimum Bend Diameters – ACI 318
Bar Size Minimum Diameter
CONCRETEPIPE.ORG
No.3 - No.8
No.9, No.10, No.11
No.14 and No.18
6db 8db 10db
db = diameter of the bar Not for Hooks or Stirrups

## Slide 35: Minimum Bend Diameters – ASTM A1064
All bends described in terms of inside diameter
Factors affecting minimum bend diameters
  Feasibility of bending without breaking
  Avoidance of concrete crushing inside the bend
Welded wire fabric
CONCRETEPIPE.ORG
W7 and smaller
Larger than W7
D6 and smaller
Larger than D6
1db 2db 2db 4db

## Slide 36: Plain Wire Splice Length – ACI 318
CONCRETEPIPE.ORG

## Slide 37: Deformed Wire Splice Length – ACI 318
CONCRETEPIPE.ORG

## Slide 38: Specifications
CONCRETEPIPE.ORG

## Slide 39: ASTM C76
Section 7.1 – Design Tables
  Tables 1 – 5
  Specify minimum required steel area
Section 7.2 – Modified/Special Designs
  Permitted for situations not covered by the design tables
  Submit proof of adequacy of the design
  Must be approved by the owner
CONCRETEPIPE.ORG

## Slide 40: ASTM C76
Section 8.1.5 – Circ. Wire Spacing
  Based on wall thickness
  4” Max for up to 4” wall thickness
  Equal to wall thickness for 4” – 6” wall thickness
  6” absolute maximum
What Is A Proper Number Of Longitudinals?
Section 8.2 – Longitudinals
  Not specified , must contain sufficient longitudinal bars or members, to maintain the reinforcement in shape and in position within the form
CONCRETEPIPE.ORG

## Slide 41: ASTM C76
Section 8.1
What Is A “Line” Of Reinforcement & What Is A “Layer” Of Reinforcement?
  A “Line” may be made of a single Layer or multiple Layers
  Two layers allowed for pipe wall less than 7”
  Three layers allowed for pipe wall 7” or larger
  Layers separated by maximum thickness of one longitudinal + 1/4”
CONCRETEPIPE.ORG

## Slide 42: ASTM C76
Section 8.1.1 - Single Cage
  Placed 35% - 50% of wall thickness from inside wall
  Pipe with wall thickness <2 1/2”, Cover = 3/4”
Section 8.1.2 - Double Cage
  Circular Cages - Concrete cover = 1”
Section 8.1.3 – Elliptical Cage
  Elliptical Cages – Cover = 1” from wall in tension (3/4” for wall < 2 1/2”)
Section 8.1.4
  Location of reinforcement subject to permissible variations of Section 12.5
CONCRETEPIPE.ORG

## Slide 43: ASTM C76
Section 12.5 - Permissible Variations
  Position of reinforcement, +/- 10% of wall thickness, or +/- 1/2” whichever is greater
If your cage is outside this permissible variation, is the pipe automatically rejected?
  Variations exceeding those above shall be accepted if D-load passes
  Must maintain minimum cover requirements (1/2” from any surface except: 1/4” from end of spigot, mating surfaces of nonrubber gasket joints or gasket groove)
CONCRETEPIPE.ORG

## Slide 44: ASTM C76
Section 8.3 - Joint Reinforcement
Non-rubber gasket joint
  For pipe 36” & larger, either the bell or spigot shall contain circumferential reinforcement
Rubber gasket joint
  For pipe 12” & larger, the bell ends shall contain circumferential reinforcement
CONCRETEPIPE.ORG

## Slide 45: ASTM C76
Section 8.1.8 - Splices
Welding
  Lap = min 2”, and a weld of sufficient length that pull test = at least 50% of min specified tensile strength of the steel
  butt-welded splices permitted only with helically wound cages, Strength = 75% of min specified strength of the steel
Lapping
  Lap = 20/40 Bar Diameters (Deformed/Plain)
  WWR lap must contain a longitudinal
CONCRETEPIPE.ORG

## Slide 49: ASTM C478
Sections 6.4.1 and 6.4.2 contain the same wording as for Sections
8.1.8 and 8.1.8.1 of ASTM C76
CONCRETEPIPE.ORG

## Slide 50: ASTM C76
Spacers & Chairs
How many spacers/chairs should you have & where should they be placed?
Section 8.2
  The exposure of the ends of longitudinals, stirrups, or spacers that have been used to position the cages during the placement of the concrete shall not be a cause for rejection.
Use enough to maintain the cage in place!
CONCRETEPIPE.ORG

## Slide 51: ASTM C1433/1577
Section 7 – Design
  Design Tables
  Modified/Special designs are allowed
  Circ. Spacing = 2”–4”, Long spacing = 8” max
Section 7.3 – Placement of Reinforcement
  Subject to permissible variations of Section 12
Section 7.4 – Laps & Welds
  All splices made by lapping
  Beware the Restricted Welding Zones!
CONCRETEPIPE.ORG

## Slide 52: ASTM C1433/1577
Section 7.4 – Laps
  The overlap measured between the outermost longitudinal wires of each fabric sheet shall not be less than the spacing of the longitudinal wires plus 2 in. but not less than 10 in.
CONCRETEPIPE.ORG

## Slide 53: ASTM C1433/1577
Do you know the Restricted Welding Zones?
CONCRETEPIPE.ORG

## Slide 54: What Makes a Good Cage?
Right Steel Areas (Circumferential & Longitudinal)
Correct Cage Dimensions
Proper Lap &/or Good Welds
Proper Spacers & Chairs
Meet Specifications
CONCRETEPIPE.ORG

## Slide 55: Thank You
Jake Jyrkama, P.E. Jaakko.Jyrkama@RinkerPipe.com